| Exp No. | Input |  |  |  |  | Output or parameter to be predicted |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Pulse On Time (Âµs) | Pulse Off Time (Âµs) | Servo Voltage (V) | Applied Current (A) | Angle of wire | Surface Roughness, Ra (Âµm) | Material Removal Rate (mm3/min) | Kerf Width(mm) |
| 1 | 12 | 12 | 55 | 4 | 60 | 4.137 | 5.866 | 1.378 |
| 2 | 12 | 12 | 60 | 3.5 | 60 | 3.752 | 5.556 | 1.277 |
| 3 | 8 | 14 | 70 | 5 | 30 | 2.458 | 4.770 | 0.943 |
| 4 | 8 | 14 | 50 | 5 | 90 | 3.795 | 5.695 | 1.289 |
| 5 | 12 | 12 | 55 | 4 | 60 | 4.225 | 5.957 | 1.400 |
| 6 | 12 | 12 | 60 | 3.5 | 60 | 3.782 | 5.653 | 1.286 |
| 7 | 8 | 10 | 70 | 5 | 90 | 2.692 | 4.919 | 1.004 |
| 8 | 8 | 14 | 70 | 5 | 30 | 2.542 | 4.838 | 0.965 |
| 9 | 12 | 13 | 60 | 4 | 60 | 3.561 | 5.442 | 1.227 |
| 10 | 8 | 14 | 50 | 5 | 90 | 3.885 | 5.773 | 1.311 |
| 11 | 16 | 10 | 70 | 5 | 30 | 3.431 | 5.540 | 1.194 |
| 12 | 16 | 10 | 70 | 3 | 90 | 3.195 | 5.021 | 1.135 |
| 13 | 8 | 10 | 70 | 5 | 90 | 2.777 | 5.024 | 1.026 |
| 14 | 12 | 13 | 60 | 4 | 60 | 3.645 | 5.535 | 1.249 |
| 15 | 16 | 10 | 70 | 5 | 30 | 3.529 | 5.643 | 1.219 |
| 16 | 16 | 10 | 70 | 3 | 90 | 3.279 | 5.172 | 1.155 |
| 17 | 12 | 12 | 60 | 4.5 | 60 | 3.859 | 5.736 | 1.305 |
| 18 | 12 | 12 | 60 | 4.5 | 60 | 3.774 | 5.644 | 1.283 |
| 19 | 16 | 14 | 50 | 3 | 90 | 4.577 | 5.901 | 1.489 |
| 20 | 16 | 14 | 50 | 3 | 90 | 4.487 | 5.797 | 1.467 |
| 21 | 8 | 14 | 70 | 3 | 90 | 2.209 | 4.290 | 0.879 |
| 22 | 8 | 14 | 70 | 3 | 90 | 2.285 | 4.393 | 0.898 |
| 23 | 14 | 12 | 60 | 4 | 60 | 4.026 | 5.785 | 1.347 |
| 24 | 14 | 12 | 60 | 4 | 60 | 3.937 | 5.683 | 1.325 |
| 25 | 12 | 12 | 65 | 4 | 60 | 3.331 | 5.338 | 1.169 |
| 26 | 12 | 12 | 65 | 4 | 60 | 3.415 | 5.440 | 1.191 |
| 27 | 8 | 10 | 50 | 3 | 30 | 4.829 | 6.589 | 1.556 |
| 28 | 12 | 12 | 60 | 4 | 75 | 3.638 | 5.517 | 1.249 |
| 29 | 12 | 11 | 60 | 4 | 60 | 3.925 | 5.752 | 1.322 |
| 30 | 8 | 10 | 50 | 3 | 30 | 4.910 | 6.668 | 1.576 |
| 31 | 12 | 12 | 60 | 4 | 75 | 3.725 | 5.620 | 1.272 |
| 32 | 12 | 11 | 60 | 4 | 60 | 4.017 | 5.850 | 1.347 |
| 33 | 16 | 10 | 50 | 5 | 90 | 5.060 | 6.577 | 1.615 |
| 34 | 16 | 10 | 50 | 5 | 90 | 4.944 | 6.467 | 1.584 |
| 35 | 16 | 14 | 70 | 3 | 30 | 2.963 | 4.848 | 1.074 |
| 36 | 16 | 14 | 70 | 3 | 30 | 3.042 | 4.950 | 1.093 |
| 37 | 16 | 14 | 50 | 5 | 30 | 4.722 | 6.258 | 1.528 |
| 38 | 16 | 14 | 50 | 5 | 30 | 4.812 | 6.331 | 1.551 |
| 39 | 12 | 12 | 60 | 4 | 45 | 3.895 | 5.773 | 1.314 |
| 40 | 12 | 12 | 60 | 4 | 45 | 3.808 | 5.684 | 1.291 |
| 41 | 10 | 12 | 60 | 4 | 60 | 3.531 | 5.519 | 1.222 |
| 42 | 10 | 12 | 60 | 4 | 60 | 3.612 | 5.614 | 1.241 |

Table 5: Hyperparametrs for optimized models

| Output | XGB Hyperparameter | XGB R² | SVR Hyperparameter | SVR R² | RF Hyperparameter | RF R² | NN Hyperparameter | NN R² |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Surface Roughness | learning_rate=0.05, max_depth=4, min_child_weight=3, n_estimators=200, subsample=0.8, colsample_bytree=0.8 | 0.904 | C=50, epsilon=0.1, gamma='scale' | 0.883 | n_estimators=300, max_depth=10, max_features='sqrt' | 0.870 | hidden_layers=(8,4,2), learning_rate_init=0.01, activation='relu' | 0.887 |
| MRR | learning_rate=0.05, max_depth=4, min_child_weight=3, n_estimators=200 | 0.875 | C=50, epsilon=0.1, gamma='scale' | 0.859 | n_estimators=300, max_depth=10 | 0.840 | hidden_layers=(6,5,4), learning_rate_init=0.01, activation='relu' | 0.831 |
| Kerf | learning_rate=0.05, max_depth=4, min_child_weight=3, n_estimators=200 | 0.918 | C=40, epsilon=0.05, gamma='scale' | 0.877 | n_estimators=300, max_depth=10 | 0.888 | hidden_layers=(5,4,3), learning_rate_init=0.01, activation='relu' | 0.755 |

| Ensemble Model Performance Summary |  |  |  |
| --- | --- | --- | --- |
| Target | RMSE | MAE | R² |
| Surface Roughness | 0.2098 | 0.1275 | 0.9088 |
| MRR | 0.1840 | 0.1110 | 0.8826 |
| Kerf Width | 0.0521 | 0.0317 | 0.9203 |

Table 6: Ensemble Model performance.

Surface Roughness

- (b)                                                              (c)

(d)                                                       (e)                                                                     (f)

(g)                                                            (h)                                                                (i)

(j)                                                         (k)                                                               (l)

FIG: Ensemble Surface Roughness Model Performance(a) Bootstrap(b) Density curve (c) Actual vs Predicted value(d)Distribution(e)Parameter Space Analysis(f) Leave-One-Out Cross-Validation(g)Heatmap(h)Epoch(i)Learning Curve(j) Validation of model with experimental value(k) Random Forest Feature Importance (l) Correlation Matrix

MRR

- (b)                                                              (c)

(d)                                                       (e)                                                                     (f)

(g)                                                          (h)                                                                (i)

(j)                                                         (k)                                                               (l)

FIG: Ensemble MRR Model Performance(a) Bootstrap(b) Density curve (c) Actual vs Predicted value(d)Distribution(e)Parameter Space Analysis(f) Leave-One-Out Cross-Validation(g)Heatmap(h)Epoch(i)Learning Curve(j) Validation of model with experimental value(k) Random Forest Feature Importance (l) Correlation Matrix

Kerf Width

- (b)                                                              (c)

(d)                                                       (e)                                                                (f)

(g)                                                         (h)                                                                (i)

(j)                                                             (k)                                                               (l)

FIG: Ensemble MRR Model Performance(a) Bootstrap(b) Density curve (c) Actual vs Predicted value(d)Distribution(e)Parameter Space Analysis(f) Leave-One-Out Cross-Validation(g)Heatmap(h)Epoch(i)Learning Curve(j) Validation of model with experimental value(k) Random Forest Feature Importance (l) Correlation Matrix

| Table 3: Optimal AWJM Process Parameter |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min Kerf | Max MRR | Balanced |
| Pulse On (µs) | 8 | 12 | 8 |
| Pulse Off (µs) | 14 | 11 | 10 |
| Servo Voltage (V) | 50 | 60 | 50 |
| Current (A) | 3 | 4 | 3 |
| Angle (°) | 90 | 75 | 30 |
| MRR (mm³/min) | 4.290 | 6.668 | 6.589 |
| Kerf Width (mm) | 0.879 | 1.576 | 1.556 |

| Table 3: Optimal AWJM Process Parameter |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min Ra | Max MRR | Balanced |
| Pulse On (µs) | 8 | 12 | 12 |
| Pulse Off (µs) | 14 | 11 | 13 |
| Servo Voltage (V) | 50 | 60 | 60 |
| Current (A) | 3 | 4 | 4 |
| Angle (°) | 90 | 75 | 30 |
| Surface Roughness (Âµm) | 2.209 | 4.910 | 3.284 |
| MRR (mm³/min) | 4.29 | 6.668 | 5.643 |

| Table 3: Optimal AWJM Process Parameter |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min Ra | Min Kerf | Balanced |
| Pulse On (µs) | 8 | 8 | 8 |
| Pulse Off (µs) | 14 | 14 | 14 |
| Servo Voltage (V) | 50 | 50 | 50 |
| Current (A) | 3 | 3 | 3 |
| Angle (°) | 90 | 90 | 90 |
| Surface Roughness (Âµm) | 2.209 | 2.209 | 2.209 |
| Kerf Width (mm) | 0.879 | 0.879 | 0.879 |